# II B. Tech. I Semester Regular Examinations– January, 2023

# MATERIALS SCIENCE AND METALLURGY

# Time: 150 Min                                         (MECH)                                      Max. Marks: 80M

# SECTION – A

Answer all Four questions					                                4×10M=40M

- For a 99.6 wt% Fe - 0.40 wt% C steel at a temperature just below the eutectoid, determine the following:

(a) The compositions of Fe3C and ferrite (α).

(b) The amount of cementite (in grams) that forms in 100 g of steel.

(c) The amounts of pearlite and proeutectoid ferrite (α) in the 100 g.

- Differentiate the mechanisms involved in three strengthening techniques and emphasize on how dislocations are involved in each of the technique.

- From Isothermal transformation diagram for an Iron – Carbon alloy of eutectoid composition sketch and label time-temperature paths to produce the following microstructures:

(a) 100% Course Pearlite

(b) 50% Martensite and 50% Austenite

(c) 50% Course Pearlite, 25% Bainite and 25% Martensite

  - Contrast the mechanical characteristics of matrix and dispersed phases for fiber reinforced composites.

SECTION-B

Answer all Two questions						                    2×20M=40M

  - Enumerate the characteristics for selecting metal powders towards the fabrication of filters and gears. Justify for choosing optimum parameters for the fabrication of components. Choose a material for fabrication and design the process to fabricate these components.

  - (a) Describe the following heat treatment procedures for steels and for each, the intended final microstructures and mechanical properties: Full Annealing, Normalizing, Quenching and Induction Hardening.

(b) Describe the simplest heat treatment procedure that would be used in converting a 0.8 wt% C steel from one microstructure to the other, as follows:

(i) Martensite to Spheroidite

(ii) Spheroidite to Martensite

(iii) Bainite to Pearlite

(iv) Pearlite to Spheroidite